## Slide 1
Inha University, Dept. of Physics
Quantum Functional Materials Lab..
이동우a, 정동근a, 김종훈b,c, 김현수a,f,
Murillo Gonzalog, 이관형b,c,d,e, 송현철f, 정종훈1
a Department of Physics, Inha University
b Department of Materials Science and Engineering, Seoul National University
c Research Institute of Advanced Materials (RIAM), Seoul National University
d Institute of Engineering Research, Seoul National University
e Institute of Applied Physics, Seoul National University
f Center for Electronic Materials, Korea Institute of Science and Technology (KIST)
g Department of Nano and Microsystems, Instituto de Microelectronica de Barcelona
Polarization-controlled PVDF-based hybrid nanogenerator
for an effective vibrational energy harvesting from human foot

## Slide 2
Outline
Ⅰ. Motivation
Triboelectric and piezoelectric nanogenerator
PVDF properties
PVDF based triboelectric and piezoelectric nanogenerator
Ⅱ. Results and discussion
PVDF based triboelectric nanogenerator & piezoelectric nanogenerator
Triboelectric and piezoelectric hybrid generator
Vibrational energy harvesting from human foot
Ⅲ. Conclusion

## Slide 3
↑
↑
Motivation : Triboelectric and piezoelectric nanogenerator
Piezoelectric nanogenerator (PENG)
Triboelectric nanogenerator (TENG)
↑
Dielectric
Electrode
Charge
↑
Pressing
Releasing
↑
↑
Releasing
↑
↑
Pressing
+
-
-
-
-
-
+
+
+
+
-
+
-
+
-
+
-
+
p
-
+
-
+
-
+
+
-
-
+
-
+
-
+
+
-
p
Piezo Material
Electrode
Polarization

## Slide 4
Motivation : PVDF Properties
Chemical structure of β-phase PVDF
Dipole ↑
Dipole ↓
Q-D. Shen et al., Adv. Electronic Mater. (2017).
PVDF’s three phases
Fluorine
Hydrogen
Carbon
β-phase PVDF
(Ferroelectric Phase)
α-phase PVDF
γ-phase PVDF
PVDF Triboelectric series
Q. Tang et al., Nano Energy (2020).

## Slide 5
Motivation : PVDF based triboelectric and piezoelectric nanogenerator
PVDF based piezoelectric nanogenerator
PVDF based triboelectric nanogenerator
P. Bei et al., Nano Research (2014).
M. Choi et al., Nano Energyt (2019).

## Slide 6
Result : PVDF based triboelectric nanogenerator & piezoelectric nanogenerator
PVDF based triboelectric nanogenerator
PVDF
Al
Al
PVDF based piezoelectric nanogenerator
PVDF
Al
Al

## Slide 7
Result : Triboelectric & piezoelectric hybrid generator

## Slide 8
Result : Triboelectric & piezoelectric hybrid generator

## Slide 9
Result : Vibrational energy harvesting from human foot

## Slide 10
Conclusion
We fabricate a PVDF film-based hybrid TP-NG in order to effectively harvest the random and irregular vibrational energy from the human foot.
The layout provides in-phase power generation from each TENG and PENG during one cycle of vibration.
The up-down polarized hybrid TP-NG generates the largest power of 20 μW/cm2 due to the modulated surface potential and ferroelectricity of PVDF.
The hybrid TP-NG sensitively generates output powers from various human motions.
In addition, the shoe insole containing TP-NG generates sufficient power to lighten LEDs and operate a wireless pressure sensor network.

## Slide 11
Thank you for listening my presentation !!!