## Slide 1: Inverse Design Method Utilizing a Hybrid Meta-heuristic Algorithm
발표자: 정인철
지도교수: 이규태

## Slide 2: Index
Meta-heuristic algorithms
Particle swarm optimization
Genetic algorithm
Differential evolution
Inverse design method
Ex1. Perfect absorber
Ex2. Transmissive color filters
Ex3. Reflective color filters
Appendix
Loss function
Glancing angle deposition
L*a*b* color space

## Slide 3: Meta-heuristic algorithms
Quicksort
Exact algorithms:
provides an exact solution
High complexity
Heuristic algorithms:
provides a good solution
Low complexity
Suitable for simple problems
Appliable for complicated problems
Traveling salesman problem

## Slide 4: Particle swarm optimization (PSO)
Particle:
particle #
iteration
Velocity:
Inertia
Cognitive
Social
Random coefficients for aggressive exploration
https://towardsdatascience.com/particle-swarm-optimization-visually-explained-46289eeb2e14

## Slide 5: Genetic algorithm (GA)
pop
pop
pop
pop
pop
pop
pop
pop
pop
pop
pop
pop
pop
pop
pop
pop
pop
pop
Next generation
Roulette wheel selection
Chart: 
| 1분기 | 2분기 | 3분기 | 4분기
판매 | 7 | 4 | 2 | 1
Run roulette wheel selection as many as the population
Survival of the fittest
Crossover
0 | 0 | 0 | 0 | 0 | 0
1 | 1 | 1 | 1 | 1 | 1
Crossover point
1 | 1 | 1 | 0 | 0 | 0
Offspring

## Slide 6: Differential evolution (DE)
Optimal
[ Initialization ]
Optimal
Mutant
[ Mutation ]
[ Crossover ]
Optimal
Trial
[ Selection ]
Optimal

## Slide 7: Inverse design of multi-layered thin films
Optimal structure
Material Sequence
Layer Thicknesses
Deposition angles
Structure developer
Optimizer
Structure developer
Optimizer
Evaluation
Structure
Optimized structure
Feedback
Particle swarm optimization (PSO)
Genetic algorithm (GA)
Differential evolution (DE)
Analogue parameters
Discrete parameters

## Slide 8: Ex1. Perfect absorber
GA-PSO | 
Loss | 0.523
Generation Reached | 51
Structure Generator | pc/pm 0.9/0.05
Structure Generator | w/c1/c2 D/0.37/0.50
HYPER PARAMETERS
Test function: Penta-layered broadband absorber utilizing glancing angle deposition
Population number: 500
Generations: 100
Wavelengths: 400~2000 nm, 5 nm interval
Materials: TiO2 (GLAD), Ge (GLAD), Cr, Ni, Mo, Ti, Au, Al, Ag
DE-PSO | 
Loss | 0.422
Generation Reached | 17
Structure Generator | F/CR 0.2/0.1
Structure Generator | w/c1/c2 D/0.37/0.50
GA-DE | 
Loss | 0.422
Generation Reached | 15
Structure Generator | pc/pm 0.9/0.05
Structure Generator | F/CR 0.2/0.1
DE-DE | 
Loss | 0.422
Generation Reached | 24
Structure Generator | F/CR 0.2/0.1
Structure Generator | F/CR 0.2/0.1
D: Dynamic
Material | Thickness (nm) | dep. ang. (°)
TiO2 | 102.7 | 84.1
TiO2 | 52.80 | 20.6
Ge | 47.66 | 74.8
Ge | 24.17 | 25.0
Cr | 217.2 | 0
Glass | 1 mm | 

## Slide 9: Ex2. Transmissive color filters
BLUE | BLUE |  | GREEN | GREEN |  | RED | RED | 
Material | Thickness | dep. ang. | Material | Thickness | dep. ang. | Material | Thickness | dep. ang.
TiO2 | 120.9 | 0.000 | TiO2 | 288.0 | 0.000 | TiO2 | 348.6 | 0.000
Ag | 29.32 |  | Ag | 32.01 |  | Ag | 27.85 | 
SiO2 | 249.2 |  | SiO2 | 134.9 |  | TiO2 | 159.8 | 81.00
Ag | 23.73 |  | Ag | 28.95 |  | Ag | 28.54 | 
TiO2 | 219.6 | 0.000 | TiO2 | 170.0 | 0.000 | Si | 20.89 | 
Glass | 1 mm |  | Glass | 1 mm |  | Glass | 1 mm | 
 | x | y | Y | Color
Filter | 0.16 | 0.06 | 0.04 | 
Ideal | 0.15 | 0.06 | 0.07 | 
Filter | 0.29 | 0.60 | 0.43 | 
Ideal | 0.30 | 0.60 | 0.72 | 
Filter | 0.61 | 0.36 | 0.14 | 
Ideal | 0.64 | 0.33 | 0.21 | 
Chart: Wavelength (nm)
Thickness: nm deposition angle: deg

## Slide 10: Ex3. Reflective color filters
Chart: Wavelength (nm)
BLUE | BLUE |  | GREEN | GREEN |  | RED | RED | 
Material | Thickness | dep. ang. | Material | Thickness | dep. ang. | Material | Thickness | dep. ang.
TiO2 | 160.8 | 31.54 | TiO2 | 91.37 | 0.000 | TiO2 | 62.58 | 71.61
SiO2 | 57.46 |  | SiO2 | 232.4 |  | Ge | 15.41 | 16.00
Ni | 13.07 |  | Cr | 9.659 |  | SiO2 | 183.6 | 
SiO2 | 130.3 |  | SiO2 | 350.7 |  | Ag | 278.9 | 
Al | 177.0 |  | Ag | 299.0 |  | Au | 66.00 | 
Glass | 1 mm |  | Glass | 1 mm |  | Glass | 1 mm | 
Thickness: nm deposition angle: deg
 | x | y | Y | Color
Filter | 0.16 | 0.06 | 0.07 | 
Ideal | 0.15 | 0.06 | 0.07 | 
Filter | 0.30 | 0.61 | 0.63 | 
Ideal | 0.30 | 0.60 | 0.72 | 
Filter | 0.60 | 0.34 | 0.20 | 
Ideal | 0.64 | 0.33 | 0.21 | 

## Slide 11: Conclusion
An inverse design method that utilizes hybrid meta-heuristic algorithm to obtain an optimized structure is demonstrated.
Since a multi-layered thin films structure consists of two different sequences, that are discrete (material sequence) and analogue (layer thickness or deposition angle).
This approach may pave a way to inverse design methods to provide diverse optical devices such as multilayered thin films, diffraction gratings, plasmonic resonance-based nano structures, and photonic crystals.

## Slide 12: Thank You!

## Slide 13: Appendix: Loss (Cost) function
Loss function:
Also called as a cost function or an error function.
A function that maps an event or values of one or more variables onto a real number intuitively representing some “cost” associated with the event.
A loss function is used for parameter estimation, and the event in question is some function of the difference between estimated and true values for an instance of data.
Mean squared error (MSE)
Root mean squared error (RMSE)
Continuous loss
Discrete loss
Cross entropy error (CEE)
Categorical cross entropy error

## Slide 14: Appendix: Glancing angle deposition (GLAD)
Substrate
Shadow effect
GLAD
Change of refractive indices of Ge according to the deposition angles
Bruggman’s model
Modified tangent rule

## Slide 15: Appendix: L*a*b* color space
[ top view ]
[ front view ]
The CIELAB color space is proposed by the International Commission on Illumination (CIE) in 1976.
CIELAB was intended as a perceptually uniform space, where a given numerical change corresponds to similar perceived change in color.
L*: Lightness value
a*: green-red opponent colors
b*: blue-yellow opponent colors